## Slide 1
QUALITY CIRCLE • QC STORY PRESENTATION
Improving Paint Appearance by
Enhancing First Time Quality
Reduction of Dust & Seed defects across the paint line — from a benchmark of 60–70 to single-digit defects per body
QC CIRCLE
PAINT PERFECTORS
DEPARTMENT
Paint Shop
THEME TYPE
Problem Solving
Prepared for the Company Quality Circle Convention
Notes: Title slide. Replace circle name PAINT PERFECTORS with your actual QC circle name. Introduce the theme and the headline result: dust/seed reduced to ~6 per body against a 60-70 benchmark seen at other plants' SOP.

## Slide 2
Our QC Circle Profile
CIRCLE IDENTITY
Circle Name
PAINT PERFECTORS [edit]
Department
Paint Shop
Date of Formation
[dd-mm-yyyy]
No. of Members
[6]
Circle Leader
[Name]
Deputy Leader
[Name]
Facilitator
[Name / Shift Engineer]
Meeting Frequency
Weekly (30 min)
MEMBERS
1
[Member 1] — Leader
2
[Member 2]
3
[Member 3]
4
[Member 4]
5
[Member 5]
6
[Member 6]
PROJECT MILESTONES
Pre-SOP
Preventive actions taken
Mid-June
Line SOP started
SOP+2 wk
Dust stabilised to single digit
Now
Sustaining & horizontal deployment
Paint Shop Quality Circle | QC Story
2
Notes: Fill in the real circle name, members, leader, and formation date. The milestone strip tells the story: preventive actions BEFORE SOP, then SOP in mid-June, then quick stabilisation to single-digit dust.

## Slide 3
The QC Story — Our Roadmap
We followed the standard QC Story problem-solving sequence and applied all seven QC tools along the way.
1
Theme Selection
Why this problem
2
Present Situation
Grasp the facts
3
Target Setting
Define success
4
Analysis
Find root causes
5
Countermeasures
Act at source
6
Results
Confirm effect
7
Standardisation
Hold the gain
8
Reflection
Learn & plan next
7 QC TOOLS USED: Check Sheet • Pareto • Cause & Effect • Histogram • Scatter • Graph / Control Chart • Stratification
Paint Shop Quality Circle | QC Story
3
Notes: Walk the panel quickly through the 8 QC-Story steps. Emphasise that this is a disciplined, tool-driven approach, and preview the seven QC tools shown in the banner.

## Slide 4
Paint Shop Process — Where Quality Is Built
Flow Chart: the body travels through Pre-treatment/ED → Sealer → Top Coat before Inspection. Dust & seed defects are caught at Inspection but originate across ED and Top Coat.
1 ED & PRE-TREATMENT
Degreasing & hot-water rinse
Surface conditioning + Phosphate
Water rinses
ED coat (1st layer) → ED bake
2 SEALER
PVC sealer application
Under-body / joint sealing
Sealer bake
3 TOP COAT
Preparation: wiping + air blow (tack-off)
Primer application
Base coat
Clear coat
DOWNSTREAM
INSPECTION
Operators check every body
REPAIR
Rectify defects found
ASSEMBLY
Dispatch to trim line
Every repair = lost First Time Quality
Paint Shop Quality Circle | QC Story
4
Notes: Note: 'Primer application' is what was described as the coat before base coat — please confirm the exact in-plant term (primer / mid-coat). Explain that dust and seed can attach anywhere from ED to clear coat, and each one caught at inspection forces a repair, which is what hurts First Time Quality.

## Slide 5
1
STEP 1 Theme Selection
WHY WE SELECTED THIS THEME
1
Customer impact — Paint appearance is the first thing a customer sees — dust & seed directly hurt perceived quality.
2
First Time Quality — Each defect forces rework, pulling down First Time Quality (FTQ) and line throughput.
3
Cost of poor quality — Repair consumes man-hours, sanding/polishing material and paint — pure waste.
4
New line, high stakes — Other plants saw 60–70 dust defects/body at SOP; a shaky start is hard to recover.
5
Aligned to goals — Directly supports the plant's quality, cost and delivery objectives.
OUR THEME
Improve paint appearance by enhancing First Time Quality through dust & seed reduction
VISION
A world-class paint finish — Right First Time, every body, every time.
MISSION
Eliminate paint defects at source through teamwork, data and the QC approach to reach best-in-class FTQ.
SLOGAN
“Right First Time — the Shine that Defines.”
Paint Shop Quality Circle | QC Story
5
Notes: This is the 'vision' the user asked for. Present vision/mission/slogan as the circle's north star, then justify the theme with the 5 reasons — lead with customer impact and First Time Quality.

## Slide 6
2
STEP 2 Present Situation
We collected defect data body-by-body (Check Sheet), then used a Pareto Diagram and Stratification to find the vital few.
PARETO — Paint Defects by Type
Dust & Seed alone = 48% of all defects
Chart: 
| Dust & Seed | Dirt / Fiber | Crater | Sag / Run | Orange Peel | Water Mark | Others
Defect Count | 48 | 18 | 12 | 9 | 7 | 4 | 2
Cumulative % | 48 | 66 | 78 | 87 | 94 | 98 | 100
CHECK SHEET (extract)
Area | Shift A | Shift B | Shift C
ED / PT | 3 | 4 | 5
Sealer | 1 | 1 | 2
Top Coat | 6 | 7 | 9
STRATIFICATION — key findings
Top Coat contributes the most dust & seed
Shift C higher — links to environment/housekeeping
Upper body (roof, hood) worse than lower body
Paint Shop Quality Circle | QC Story
6
Notes: Charts use illustrative numbers — replace with your real defect counts. The Pareto proves Dust & Seed is the 'vital few' worth attacking. Stratification shows it concentrates in Top Coat, on Shift C, upper body — pointing to environment and method.

## Slide 7
3
STEP 3 Target Setting
OUR TARGET
Reduce Dust & Seed defects per body (DPB) to single digit from the first day of SOP.
What
Dust & Seed defects / body
From
60–70 (other plants at SOP)
To
≤ 10, stretch ≤ 6
By
Within 2 weeks of SOP
How
Preventive actions at source
BENCHMARK → TARGET → ACHIEVED
Dust & Seed defects per body
Chart: 
| Other plants @ SOP | Our Target | Our Stretch | Achieved
DPB | 65 | 10 | 6 | 6
Paint Shop Quality Circle | QC Story
7
Notes: Frame the target against the external benchmark: other plants hit 60-70 at SOP; we set a single-digit target and achieved 6. Replace numbers with your actual target and result.

## Slide 8
4
STEP 4 Analysis — Cause & Effect (Fishbone)
High
Dust & Seed
Defects
MAN
Wiping / painting technique
Housekeeping discipline
MACHINE
Magnet rod fouling in tanks
Magnetic filter loading
ED / phosphate sludge
MATERIAL
ED paint NV variation
Contaminated rinse water
Lint-shedding consumables
METHOD
Poor tack-off (wipe + air blow)
Painting sequence drops dust
Rinse cycle not optimised
ENVIRONMENT
Airborne dust from storage
Open joints / gaps in line
Dust settling on body
MEASUREMENT
Infrequent bath-parameter checks
Paint Shop Quality Circle | QC Story
8
Notes: The 6-M fishbone for dust & seed. Walk each bone. Note the three heavy branches — Environment, Machine/Material (bath cleanliness) and Method/Man — which map directly to our three countermeasures.

## Slide 9
4
STEP 4 Analysis — Root Causes Confirmed
Why-Why analysis and data (Scatter Diagram + Histogram) confirmed the vital root causes.
CONFIRMED ROOT CAUSES
1
Airborne dust from uncovered storage & open line joints settling on wet paint
2
Metal fines / sludge in ED & phosphate tanks (magnet rods & filters not cleaned often enough)
3
ED bath NV drift causing ED drops / runs and extra repair
4
Lint-shedding wipes and non-standard painting sequence adding fibre & dust in Top Coat
SCATTER
Airborne dust vs seed defects
Chart: Airborne dust count
| 12 | 18 | 22 | 28 | 33 | 39 | 45 | 52 | 58 | 64 | 70 | 20 | 30 | 48 | 60
Seed defects/body | 3 | 5 | 6 | 8 | 10 | 12 | 16 | 20 | 24 | 28 | 33 | 6 | 9 | 18 | 26
Strong positive correlation → control dust, control defects
HISTOGRAM
Defects/body distribution (early SOP)
Chart: 
| 0-3 | 4-6 | 7-9 | 10-12 | 13-15 | 16+
Bodies | 6 | 14 | 20 | 12 | 6 | 3
Spread was wide & shifted high → unstable process
Paint Shop Quality Circle | QC Story
9
Notes: Scatter proves dust drives seed defects (justifies environment countermeasure). Histogram shows the early distribution was wide and shifted high — an unstable process needing action. Numbers illustrative; replace with actuals.

## Slide 10
5
STEP 5 Countermeasures — Three Major Actions
CM-1
Environmental
Dust Control
Stop dust before it reaches the body
Storage covered with green net + aluminium foil
All joints & gaps taped/sealed
Housekeeping discipline raised
CM-2
ED & Pre-treatment
Quality
Clean baths = clean surface, fewer ED drops
Magnet-rod cleaning frequency ↑ in sub-tanks
Magnetic filter cleaning ↑
Phosphate sludge reduced, ED bath NV controlled
CM-3
Top Coat Consumables
& Operator Method
Zero-lint materials + right sequence
Indirect consumables changed to lint-free / tack cloth
Painting & tack-off sequence standardised
Prep (wipe + air blow) reinforced
Paint Shop Quality Circle | QC Story
10
Notes: These are the three major countermeasures the user asked to land near the end. Each attacks a root-cause cluster from the fishbone. The next three slides detail each one.

## Slide 11
Countermeasure 1 — Environmental Dust Control
CM-1
Root cause: airborne dust from storage & open joints settling on wet paint
1
Covered material storage
All stored parts / racks covered with green net and aluminium foil to trap and block settling dust.
2
Sealed joints & gaps
Tapes applied at line joints, panel gaps and openings so environmental dust cannot fall onto the body.
3
Housekeeping & discipline
Tightened cleaning routine and entry discipline in the paint area, especially on the weaker shift.
IMPACT
Removes the single biggest source of seed on the paint surface — dust never reaches the wet film.
KEY DEFECTS ADDRESSED
Seed / dust inclusions
Fibre on clear coat
Random surface dirt
Paint Shop Quality Circle | QC Story
11
Notes: CM-1 detail. Tie back to the scatter diagram: reducing airborne dust directly reduces seed. Add before/after photos of the netting/foil covers and taped joints if available.

## Slide 12
Countermeasure 2 — ED & Pre-treatment Quality
CM-2
Root cause: metal fines / sludge in baths and ED bath NV drift
1
Magnet-rod cleaning ↑
Increased cleaning frequency of magnet rods in the sub-tanks to pull out metal fines before ED.
2
Magnetic filter cleaning ↑
Stepped up magnetic filter cleaning so trapped particles don't recirculate into the bath.
3
Phosphate sludge reduced
Actions to cut phosphate sludge generation & carry-over across rinses (hot water, surface conditioning, water rinses).
4
ED bath NV controlled
Held ED paint NV (non-volatile) in band to stabilise film and cut ED drops / runs — reducing avoidable repair.
IMPACT
A cleaner, more stable ED foundation means fewer defects carried into Top Coat and fewer ED drops.
RESULT
Better ED film level
Fewer ED drops → less repair
Lower defect carry-over
Paint Shop Quality Circle | QC Story
12
Notes: CM-2 detail. Confirm the term 'NV' (non-volatile content of the ED bath) matches your plant's wording. Highlight the maintenance-frequency changes (magnet rods, magnetic filters) as low-cost, high-impact actions.

## Slide 13
Countermeasure 3 — Top Coat Consumables & Method
CM-3
Root cause: lint-shedding consumables & non-standard painting sequence
1
Lint-free consumables
Indirect consumables (wiping cloths / gloves / tack rags) changed to lint-free, low-shed materials so no fibre transfers to the body.
2
Standardised painting sequence
Operator painting motion & gun sequence revised so movement does not disturb or drop dust onto freshly painted panels.
3
Reinforced preparation
Wiping + air-blow tack-off before paint strengthened to remove loose particles at the last moment.
IMPACT
The last line of defence: clean materials and clean movement keep the finished surface defect-free.
KEY DEFECTS ADDRESSED
Fibre / lint marks
Dust in base & clear coat
Handling-induced dirt
Paint Shop Quality Circle | QC Story
13
Notes: CM-3 detail. 'Lint-free / tack cloth' is my read of the described consumable change ('lint free and Zoombots') — confirm the exact product name. Emphasise this is the final safeguard right before and during application.

## Slide 14
6
STEP 6 Results — Confirming the Effect
DUST & SEED / BODY
6
vs 60–70 at other plants' SOP
~90% BETTER
than the SOP benchmark
FTQ improved at SOP
Fewer bodies to repair
ED drops reduced
BENCHMARK COMPARISON
Chart: 
| Other plants @ SOP | Our line @ SOP
DPB | 65 | 6
STABILISATION TREND
Graph / Control Chart — DPB by week
Chart: 
| W1 | W2 | W3 | W4 | W5 | W6 | W7
DPB | 12 | 9 | 7 | 6 | 6 | 5 | 6
Paint Shop Quality Circle | QC Story
14
Notes: The payoff slide. Numbers are illustrative placeholders — drop in your real DPB, weekly trend and any target line. Mention tangible benefits (repair man-hours, material saved) and intangibles (team confidence, discipline).

## Slide 15
Seven QC Tools — How We Used Them
1
Check Sheet
Recorded defects body-by-body by area & shift
2
Pareto Diagram
Ranked defect types — Dust & Seed = the vital few
3
Cause & Effect
6-M fishbone to find root causes of dust & seed
4
Histogram
Showed defects/body spread was wide & unstable
5
Scatter Diagram
Confirmed dust count drives seed defects
6
Graph / Control Chart
Tracked weekly DPB & benchmark comparison
7
Stratification
Split data by area, shift & body zone
All 7 tools, one story
Data-driven from problem to proof — the backbone of our QC Story.
Paint Shop Quality Circle | QC Story
15
Notes: Reinforcement slide showing the panel that all seven QC tools were genuinely applied and where. Good slide to pause on for a judging criterion around tool usage.

## Slide 16
7
STEP 7 Standardisation — Holding the Gain
Every effective countermeasure was locked into the system so the improvement sticks and can be copied.
1
SOP / Work Instructions
Painting & tack-off sequence, wiping and prep steps documented and trained to all operators.
2
Preventive Maintenance
Magnet-rod & magnetic-filter cleaning frequency added to the PM checklist with defined intervals.
3
Bath Control Plan
ED NV, phosphate & rinse parameters put on a monitoring/reaction plan with clear limits.
4
Environment Standard
Storage covering (net/foil) and joint sealing made a daily housekeeping standard & audit point.
5
Consumable Specification
Only approved lint-free consumables allowed; specified in the purchase/issue standard.
6
Horizontal Deployment
Learnings shared with other lines/plants to prevent the 60–70 SOP problem elsewhere.
Paint Shop Quality Circle | QC Story
16
Notes: Standardisation = how we prevent recurrence. Stress PM frequency, control plan limits, the environment audit point, and horizontal deployment to sister plants.

## Slide 17
8
STEP 8 Reflection & Future Plans
WHAT WE LEARNED
✓
Preventing defects before SOP beats chasing them after — proactive wins.
✓
Environment control is as critical as paint parameters for appearance.
✓
Simple maintenance-frequency changes gave large, low-cost gains.
✓
Data & the 7 QC tools turned opinions into confirmed root causes.
✓
Teamwork across all shifts sustained the result.
NEXT TARGETS
1
Drive DPB below 5
Push dust & seed even lower and tighten the distribution.
2
Tackle next defect
Apply the same QC Story to the next Pareto item (dirt/fibre, crater).
3
Sustain & audit
Layered audits to keep environment & bath standards in place.
4
Extend horizontally
Roll the standards to all lines and future SOPs.
Paint Shop Quality Circle | QC Story
17
Notes: Close the loop: reflect honestly on learnings and commit to the next cycle — this shows the panel the circle keeps improving (PDCA never stops).

## Slide 18
THANK YOU
“Right First Time — the Shine that Defines.”
From 60–70 to single-digit dust & seed defects per body — First Time Quality, built in at source.
PAINT PERFECTORS • Paint Shop Quality Circle • Questions welcome
Notes: Closing slide. End on the slogan and the headline result, then invite questions from the panel.