SUPPLIER VISIT REPORT

Investigation of PVC Sealer Nozzle Choking & Filter Contamination

Supplier: Kansai Nerolac Paints Ltd

Product: PVC Sole Sealer / PVC Seam Sealer & PVC UBB

Process Flow No. PFC/PNT/16

Confidential — For Internal Quality Use

# Document Control

| Report No. | SVR / PVC-SEALER / 2026-07 — [confirm reference] |
| --- | --- |
| Report Date | 27 July 2026 |
| Date of Visit | [to be filled] |
| Supplier / Vendor | Kansai Nerolac Paints Ltd — [plant / location] |
| Product | PVC Sole Sealer, PVC Seam Sealer & PVC UBB (Process Flow No. PFC/PNT/16) |
| Application | Automotive body sealing in paint shop — robotic applicators (1 mm nozzle) + manual guns |
| Subject / Concern | Recurring choking of 1 mm robotic applicator nozzles; contaminant flakes retained on filters |
| Visit Team | [names / functions — Customer Quality, SQA, Process Engineering] |
| Supplier Representatives | [names / functions — Production, QA/QC, PE] |
| Prepared By | [name / designation] |
| Distribution | Customer Quality • SQA • Paint Shop • Supplier QA |

# 1.  Purpose & Scope

Establishes the root cause of recurring 1 mm robotic nozzle choking during paint-shop sealer application and agrees corrective actions with the supplier, Kansai Nerolac Paints Ltd. Scope: process review (raw material to dispatch), shop-floor observation, sampling across operations, and FTIR of the choke material versus source samples.

# 2.  Background & Problem Statement

Drum-supplied PVC sealer is applied to vehicle bodies via 1 mm robotic nozzles and manual guns. The nozzles choke intermittently and the filters retain reddish-brown, thin, layered flakes — some with embedded fibres and a foreign speck. Impact: line stoppages, nozzle cleaning, higher filter-change frequency and seal-quality risk.

## Physical evidence

- Reddish-brown, flaky / skin-like — distinct from the bulk sealer colour.

- Thin and layered — passes a coarse mesh edge-on, then bridges the 1 mm orifice.

- Embedded fibres and a foreign speck on the filter — external matter, not sealer alone.

# 3.  Product & Process Overview

The sealer is a PVC plastisol (paste resin, plasticizer, CaCO₃ filler, rheology modifier, additives). Process PFC/PNT/16 runs from RM receipt through mixing, maturation, vacuuming, viscosity correction, filtration (60# mesh), filling, testing and dispatch. Key stages:

| Op. No. | Machine / Facility | Process Description | Key Parameter |
| --- | --- | --- | --- |
| 10 | Brookfield Viscometer, Oven & Balance | Received Inspection of incoming raw material | Per RM control plan |
| 20 | Weighing Balance | Prebatching & issue of raw material | Per RM requisition |
| 30 | Fork Lift | Move to production line | Per work instruction |
| 50 | Twin Shaft Mixer (TSM) | Mixing | Temp < 35 °C; RPM/HSD per PIV |
| 60 | TSM | Ageing / Maturation | Maturation 8 hrs |
| 70 | Brookfield Viscometer | Inspection & correction | Viscosity to spec |
| 80 | TSM | Vacuuming & mixing | Vacuum 700 mmHg, 60 min |
| 90 | Brookfield Viscometer | Final viscosity adjustment | Viscosity to spec |
| 100 | Self-cleaning Filtration Unit | Filtration | Mesh 60# ; no foreign matter |
| 110 | Weighing scale | Filling & packing | Appropriate drum per PIV |
| 120 | Viscometer, Oven, Panels | Finished product testing | All parameters within spec |
| 130 | Sticker Pasting | Labelling | Batch / part / mfg. date |
| 140 | Stacker | Dispatch / delivery | Loading to truck |

Note: in-line filtration is 60# (≈ 250 µm); the nozzle is 1 mm (1000 µm). A flake finer than 250 µm passes the mesh yet still bridges the orifice — so choking occurs despite nominal filtration.

# 4.  Observations During Visit

- Open transfer points (hopper, drum filling) allow airborne dust / fibre ingress.

- Hopper cleaning between batches identified as a required control (residue build-up).

- Skinning at air-exposed surfaces — drum headspace, hopper, dead-leg lines; oxidised skin is reddish-brown and flakes off.

- Packing / liner material sheds textile fibres — matches fibres on the filter.

- Dust on drum exteriors, lids and inside empty drums — a mineral-dust ingress route.

- Mixing < 35 °C and maturation time critical; excursions in process / storage / transport can pre-gel the plastisol.

- Rheology-modifier dispersion / addition sequence under supplier review — relevant to agglomerates.

# 5.  Sampling Plan

Samples were taken from operations representing possible contamination sources plus the choke material itself; each source fingerprint was compared against the reference choke sample by FTIR.

| Sample | Location / Purpose |
| --- | --- |
| Nozzle Choking Sample ✓ (reference) | The actual choke material recovered from the applicator — the fingerprint to be matched |
| Nozzle Choking Sample — Barrel Clamping | Choke material variant / second recovery point for comparison |
| Hopper Inside | Residue / skin from the mixer hopper interior |
| Dust on Drum | Dust from the drum exterior surface |
| Drum Inside Dust | Dust from inside the (empty) drum prior to filling |
| Drum Lid — Clean | Reference from a cleaned drum lid |
| Packing Bag Part | Material from the packing / liner (fibre source check) |

# 6.  FTIR Results

Overlay FTIR (transmittance) was run on all samples. Principal bands:

| Band (cm⁻¹) | Assignment | Indicates |
| --- | --- | --- |
| ~3300–3400 (broad) | O–H / N–H stretch | Moisture / hydroxyl and cellulose (packing-bag fibre / paper) |
| ~2920 / 2850 | Aliphatic C–H stretch | Plasticizer + PVC + hydrocarbon |
| ~1720 (if present) | Ester C=O | Phthalate plasticizer (product signature) |
| ~1420–1450 (deep, broad) | Carbonate ν₃ | Calcium carbonate (CaCO₃) filler |
| ~1000–1100 (deep) | Si–O–Si stretch | Silica / silicate / talc / clay (rheology modifier or mineral dust) |
| ~875 (sharp) | Carbonate ν₂ | CaCO₃ |
| ~712 (sharp) | Carbonate ν₄ | CaCO₃ (calcite) |
| ~600–690 | C–Cl stretch | PVC |

## Interpretation

- Choke fingerprint is dominated by carbonate (≈1420 / 875 / 712) and silicate (≈1000–1100) on a PVC / plasticizer / hydrocarbon backbone, with an O–H band — i.e. product blended with mineral dust and likely fibre, not a cleanly gelled product.

- Consistent with the physical evidence (flakes + fibres + speck) and the hopper-cleaning requirement.

- This is a source-tracing exercise: the best-overlapping source spectrum names the origin.

## Confirmation required

- Pairwise match / correlation index of the choke sample vs each source (report % match) — highest names the source.

- Difference spectrum (choke − clean product): carbonate / silicate / O–H residuals → dust + fibre; carbonyl shift only → skin / oxidation.

- EDS / XRF on flakes (confirms silica / clay / CaCO₃, flags Fe / rust) and TGA / ash for filler loading vs spec.

# 7.  Root Cause Analysis

Candidate causes ranked from the evidence:

| # | Root-cause hypothesis | Supporting evidence | Assessment |
| --- | --- | --- | --- |
| 1 | Contamination ingress — mineral dust (silicate / carbonate) + packing-bag fibre entering product at open hopper / drum / packing stages, agglomerating with product into flakes | FTIR carbonate + silicate + O–H; fibres & speck on filter; drum / lid / hopper dust | Most probable |
| 2 | Surface skinning — oxidised skin from air exposure at drum headspace, hopper surface, dead-leg lines and nozzle tip flaking into the material | Flaky reddish-brown layered morphology; open surfaces observed | Contributing |
| 3 | Pre-gelation — partial gelation from temperature / time excursion during processing, storage or transport (spec: mixing < 35 °C) | Temperature-sensitive plastisol; ambient / transport heat | To rule out |
| 4 | Filler / rheology-modifier agglomerates — poorly dispersed CaCO₃ or silicate lumps | Silicate band; dispersion / addition sequence under review | Secondary |

Indication: driven principally by contamination ingress and skinning at the supplier's open handling / packing stages — a containment / housekeeping issue, not a formulation defect. Rule out pre-gelation via the confirmation tests.

# 8.  Corrective & Preventive Actions (CAPA)

Agreed actions; owners and target dates to be confirmed and tracked to closure.

| # | Action | Responsibility | Target | Status |
| --- | --- | --- | --- | --- |
| 1 | Seal and clean the mixer hopper between batches; cover open transfer points to prevent airborne dust / fibre ingress | Supplier — Prod. | [date] | Open |
| 2 | De-dust drums and lids before filling; store empty drums covered; verify drum-interior cleanliness at filling | Supplier — Prod. | [date] | Open |
| 3 | Replace fibre-shedding packing / liner with a non-shedding liner; verify no fibre release | Supplier — QA | [date] | Open |
| 4 | Minimise drum headspace and eliminate dead-legs in transfer lines; control surface skinning (sealed lids / follower plate) | Supplier — PE | [date] | Open |
| 5 | Enforce mixing temperature < 35 °C and control storage / transport temperature; FIFO on stock to limit ageing | Supplier — Prod. | [date] | Open |
| 6 | Confirm root cause: pairwise FTIR match index + difference spectrum; EDS/XRF and TGA/ash on choke flakes | Supplier QA + Customer | [date] | Open |
| 7 | Review filler / rheology-modifier dispersion & addition sequence to prevent agglomerates | Supplier — PE | [date] | Open |
| 8 | Step final filtration finer than 60# and add point-of-use (last-chance) filter before the robot nozzle (80–100 mesh) | Supplier + Paint Shop | [date] | Open |
| 9 | Introduce incoming / receiving filtration & cleanliness check at paint shop; monitor filter-retained matter as a KPI | Customer — Paint Shop | [date] | Open |

# 9.  Conclusion

Nozzle choking is attributed principally to contamination ingress (mineral dust + packing fibre) with surface skinning at the supplier's open hopper / drum / packing stages, forming flakes that pass coarse filtration and bridge the nozzle; FTIR supports a dust / fibre-laden fingerprint, not a gelled-product one. The fix is containment, cleanliness and filtration control at the supplier plus point-of-use filtration at the paint shop — not reformulation. Exclude pre-gelation via the confirmation tests.

# 10.  Next Steps

- Supplier to submit a formal 8D / CAPA with confirmation analysis (pairwise FTIR match, difference spectrum, EDS/XRF, TGA/ash) naming the source.

- Agree owners / target dates per CAPA item; track to closure with effectiveness verification.

- Trial batch after containment; monitor choking frequency and filter-retained matter as the KPI.

- Follow-up re-audit of supplier housekeeping and packing controls.

## Acknowledgement / Sign-off

| Prepared by (Visit Team) | Reviewed by (Customer Quality) | Acknowledged by (Supplier) |
| --- | --- | --- |
| Name: ______________________ Designation: ________________ Signature / Date: ___________ | Name: ______________________ Designation: ________________ Signature / Date: ___________ | Name: ______________________ Designation: ________________ Signature / Date: ___________ |

Bracketed [ ] fields to be completed with visit-specific details. FTIR interpretation reflects the visible overlay; pairwise match / difference spectrum and EDS-XRF / TGA are required to confirm the exact source.